# Inspection Analysis Report

| Equipment | HX-204 |
| --- | --- |
| Analysis Date | 2026-09-10 05:32 |
| Report Type | thickness_approval |
| Generated By | Sovereign AI Workbench |
| Confidence | 88% |
| Status | REJECT |

# Findings

Wall thickness measured at 2.8 mm

Minimum required thickness is 3.5 mm

# Measurements

| Parameter | Measured | Required / Limit |
| --- | --- | --- |
| Wall Thickness | 2.8 | 3.5 |

# Deviations

Wall Thickness: -0.7 mm (Below Minimum)

# Recommendations

REJECT: Wall thickness is below required specification

CONFIDENTIAL - For Internal Use Only